Date of update: 01.04.2026

DATA SHEET

MONBAT SLI PREMIUM EN NP90L5P0_1 100 Ah

Mechanical specification

| Dimensional group: | L5 |
| --- | --- |
| ETN reference: | 600 044 092 SMF |
| DIN reference: | 60044 |
| DimensionsA in mm (LxWxH): | 353x175x190 |
| Cell Layout: | 0 |
| Terminal Type: | 1 |

According to EN 50342

| Lid | Material | Polypropylene |
| --- | --- | --- |
|  | Cover design | SMF |
|  | Colour | Grey |

Hold-down

Layout

Separator

| Type | PE |
| --- | --- |

WeightB

| Battery weight in kg: | 17.10 |
| --- | --- |
| Acid weight in kg: | 6.70 |
| Total battery weight in kg: | 23.80 |

Battery classification as per EN 50342-1

| Water consumption | Charge retention | Vibration resistance | Endurance Level |
| --- | --- | --- | --- |
| W4 | C2 | V2 | E2 |

| Handles | Material | Polypropylene |
| --- | --- | --- |
|  | Position | Top - on lid |
|  | Colour | Grey |

| Vent caps | Material | Polypropylene |
| --- | --- | --- |
|  | Type | SMF |
|  | Colour | Grey |

Container

| Case | Material | Polypropylene |
| --- | --- | --- |
|  | Bottom hold-down | B13 |
|  | Colour | Grey |

Electrical specification

| Voltage: | 12V |
| --- | --- |
| Capacity C20: | 100 Ah |
| Cold cranking current: | 900 A [EN] |
| Cold cranking current: | 920 A [SAE] |